#### Optical Properties

- Optical Transmission spectrum of BK7

- Refractive Index nd : 1,51680 (587,6nm)

- Abbe numbers:

  - ve = 63,96

  - vd = 64,17

#### Mechanical Properties

- Density: 2,51 g/cm3

- Young's modulus E: 82 x 103 N/mm2

- Poisson's ratio μ: 0,206

- Knoop hardness HK0,1/20: 610

#### Thermal Properties

- Coefficient of thermal expansion:

  - 7,1 x10-6/K (-30°C to +70°C)

  - 8,3 x10-6/K (+20 to +300°C)

- Viscosities:

  - Softening Point (107,6 dPa): 719°C

  - Annealing Point (1013 dPa): 557°C

- Transformation temperature Tg: 557°C

#### Chemical Resistances

- Climate Resistance Class 2
Resistance against humidity is expressed
by CR-Classes 1 (high) to 4 (low).

- Stain Resistance Class 0
Resistance against staining is expressed
by FR-Classes 0 (high) to 5 (low).

- Acid Resistance Class 1
Resistance against acid solutions is expressed
by SR-Classes 0 (high) to 4 (low).

- Alkali Resistance Class 2
Resistance against alkali solutions is expressed
by AR-Classes 0 (high) to 4 (low).

- Phosphate Resistance Class 2,3
Resistance against an alkali phosphate solution
is expressed by PR-Classes 1 (high) bis 4 (low