GaAs Single Crystal Substrates

Physical  Properties of GaAs. (Doped or undoped ) Crystal

Crystal structure    Zinc blende

Lattice constant:   5.65 Å

Density:                 5.32 g/cm3

Atomic density 4.5 ´ 1022 atoms/cm3

Molecular weight 144.64

Bulk modulus 7.55 ´ 1011 dyn/cm2

Sheer modulus 3.26 ´ 1011 dyn/cm2

Coefficient of thermal expansion 5.8 ´ 10–6 K–1

Specific heat 0.327 J/g-K

Lattice thermal conductivity 0.55 W/cm-°C

Dielectric constant 12.85

Band gap 1.42 eV

Threshold field 3.3 kV/cm

Peak drift velocity 2.1 ´ 107 cm/s

Electron mobility (undoped) 8500 cm2/V-s

Hole mobility (undoped) 400 cm2/V-s

Melting point 1238°C

Typical Properties for Various GaAs Wafer

| Parameters | Undoped GaAs | Si Doped GaAs | Zn Doped GaAs | Cr Doped GaAs | Te Doped GaAs |
| --- | --- | --- | --- | --- | --- |
| Growth Method | LEC or VGF | VGF | LEC or VGF | VGF | LEC at High pressure |
| Doping | Undoped | Si | Zn | Cr | Te |
| Conductor Type | N or Semi-Insulating | N | P | Semi-insulating | N |
| Carrier Concentration ( cm-3 ) | (0.4—4.4) x108 | 4.2x1016—3.1x1018 | ( 5x1018 | ______ | (1-2) x1017 |
| Resistivity ( (.cm) | ( 1x107 | (1.6-4)x 10-3 | ____ | ( 5 x107 | (0.74-1.05)x 10-2 |
| Mobility (cm2.V-1.S-1) | ( 4500 | 1670-3700 | ( 50 | 5560-5950 | ( 1500 |
| E.P.D. ( cm-2) | ( x105 | <5000 | ( 5000 | <5000 | ( 10000 |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4705   E-mail: info@mticrystal.com   Website: www.mticrystal.com