|  | II-VI Crystals > II-VI crystals are likely to shoot in prominence in the near future. Their direct band gap nature, their large range of transparency, and the availability of a wide choice of band gap offer interesting device possibilities. MTI is able to offer high quality II-V single crystals as the follows at reasonable price. Please email us at sales@mtixtl.com we will reply you within 24 hours. Properties CdS CdTe Cd 1-x ZnxTe ZnS ZnTe ZnSe Growth Mehod PVT PVT Bridgeman Bridgeman Bridgeman CVD Structure Hexagonal Cubic Cubic Cubic cubic Cubic Lattice Constant (A) a=4.1367 c=6.7161 a = 6.483 a=6.486 5.420 6.103 a= 5.6685 Density ( g/cm3) 4.821 5.851 5.851 4.08 5.633 5.264 Melting Point (oC) 1287 1047 1045 1830 1239 1517 Heat Capacity (J /g.k) 0.3814 0.210 0.210 0.469 0.16 0.339 Thermal Expans. (10-6/K) 4.6 // a 2.5 // c 5.0 5.0 6.8 8.0 7.1 Thermal Conductivity ( W /m.k at 300K ) 2.7 6.3 0.16 13 Transparent wavelength ( um) 2.5 ~ 15 (>71%) 0.85 ~ 29.9 (>66%) 2 -12 (>71%) 7 -12 (>66%) 0.51 ~ 19.0 (>71%) Refractive Index 1.708 (o) 1.723 (e) 2.72 2.4 2.7 2.5 E-OCoeff. (m/V) at 10.6 6.8x10-12 2.0x10-12 4.0x10-12 6.1x10-12 Max. size (mm ) 25x25x15 25 x 10 x 10 40 x 40 x 10 40d x40h 40d x40h 25x25x15 |
| --- | --- |