CdS     CdTe     ZnSe    ZnO

II-VI  Compound Semiconductor Crystals

With advance in doping and junction fabrication technology of II-VI semiconductors, these materials are likely to shoot in prominence in the near future.  Their direct band gap nature, their large range of transparency, and  the availability of a wide choice of band gap  offer interesting device possibilities.  However, the growth of large area single crystal remains difficult and chanllenging.  MTI is able to offer medium sized, high quality single crystal of CdS, CdTe, ZnSe and ZnO at reasonable price.

|  | CdS | CdTe | ZnSe | ZnO |
| --- | --- | --- | --- | --- |
| Growth Mehod | PVT | PVT | PVT | Hydro-thermal |
| Structure | Hexagonal P63mc | Cubic F43m | Cubic F43m | Hexagonal P63mc |
| Lattice Constant (Å) | a = 4.1367 c = 6.7161 | a = 6.483 | a = 5.6685 | a=3.325 c=5.213 |
| Mol. weight | 144.48 | 240.01 | 144.34 | 81.39 |
| Density ( g/cm3) | 4.821 | 5.851 | 5.264 | 5.605 |
| Melting Point (oC) | 1287 | 1047 | 1517 | 1975 |
| Heat Capacity (J /g.k) | 0.3814 | 0.210 | 0.339 | 0.125 cal/gm |
| Thermal Expansion (10-6 /K) | 4.6 // a 2.5 // c | 5.0 | 7.1 | 6.5 // a 3.7 // c |
| Thermal Conductivity ( W /m.k at 300K ) | 2.7 | 6.3 | 13 | 30 |
| Transparent wavelength (µ) | 0.52 ~ 14.8 | 0.85 ~ 29.9 | 0.51 ~ 19.0 | 0.4 ~ 0.6 |
| Refractive Index | 1.708 (o) 1.723 (e) | 2.72 | 2.5 | 1.922 (o) 1.936 (e) |
| Max. Crystal size (mm ) | 25x25x15 | 25 x 10 x 10 | 25x25x15 | 20x20x10 |
| Application | X-ray detector, junction devices, substrate for epitaxy, crystal pieces for evaporation source | X-ray detector; IR optics; Substrate for epitaxy; crystal pieces for evaporation source | IR optics for CO2 laser, lenses, window; Beamsplitters; Substrate for epitaxy, Crystal pieces for evaporation source | Substrate for epitaxy of GaN ( blue LED), wide band junction devices |

MTI Corporation                                                                         www.mticrystal.com

860 S 19th Street, CA 94804, Richmond, CA 94804, USA

Tel: (510)525-3070     Fax: (510)525-4705         E-mail:  xrd@mticrystal.com        online store:   www.mtixtl.com