InP

Single Crystal Substrates

MTI supplies high quality  InP single crystal wafers for semiconductor industries.  InP  crystal is grown by a special LEC technique. The wafers are cut along precise orientation and highly epi polished.

Typical Properties

| Dopant | Type | Carrier Concentration ( cm-3) | Mobility ( cm2/V.Sec) | Resistivity ( ohm-cm ) | EPD (cm-2) |
| --- | --- | --- | --- | --- | --- |
| Undoped | N | 0.8 ~ 2.0 x1015 | 3600 ~ 4000 | 0.03 ~ 0.2 | 5~6 x104 |
| Sn | N | 0.5 ~1.0 x1018 0.5 ~1.0 x1018 | 200 ~ 2400 1500 ~ 2000 | 0.001 ~ 0.002 0.0025~0.007 | 3~5 x104 |
| Zn | P | 0.8 ~ 2.0 x1018 2.5 ~ 4.0 x1018 | 2500 ~ 3500 1300 ~ 1600 | 0.0025 ~ 0.006 | 1~ 3 x104 |
| Fe | N | 0.1 ~ 1.0 | 2000 | 107 ~ 108 | 4~ 5 x104 |

Standard Products

| Products | Dimension ( mm ) | Orientation | Others |
| --- | --- | --- | --- |
| Ingot | 2” dia x 200 mm L 3” dia x 100 mm L | <100> | Purity > 99.9999% |
| epi polished wafer | 2” dia x 0.3 mm 3” dia x 0.5 mm | <100>, <110> ,<111> or customer specs | epi ready are available upon request |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com