Typical Properties of InSb Single Crystal

| Structure | Cubic Zinc Blende |
| --- | --- |
| Space Group | F bar 3m |
| Lattice Parameter a0 at 300K | 0.647 nm |
| Nearest Neighbour Distance at 300K | 0.280 nm |
| Density at 300K | 5.80 g.cm-3 |
| Elastic Modulus c11 at 300 K | . . . . |
| Linear Expansion Coeff. at 300 K | . . . . |
| LO Phonon Energy | . . . |
| TO Phonon Energy | . . . |
| Thermal Conductivity at 300 K | . . . |
| Melting Point | . . . |
| Dielectric Constant (f=0 to f=RF) | 17.7 |
| Nature of Energy Gap Eg | Direct |
| Energy Gap Eg at 300 K | 0.17 eV |
| Energy Gap Eg at ca. 0 K | 0.237 eV (at 2 K) |
| Intrinsic Carrier Conc. at 300 K | . . . . |
| Ionisation Energy of Silicon Donor | . . . . . |
| Electron Effective Mass / m0 | 0.013 (Sze 1969) |
| Electron Hall Mobility at 300 K for n = . . | . . . . |
| Electron Hall Mobility at 77 K for n = . . | . . . . |
| Ionisation Energy of Zinc Acceptor | . . . . . |
| Light Hole Effective Mass mlh/m0 | . . . |
| Heavy Hole Effective Mass mhh/m0 | . . . |
| Hole Density of States Mass mdos/m0 | 0.4 (Singh 1993) |
| Hole Hall Mobility at 300 K for p = . . . cm-3 | . . . . |
| Hole Hall Mobility at 77 K for p = . . . cm-3 | . . . . |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com