Typical Properties

Molecular weight			:	268.04

Crystal Structure			:	Cubic, Perovskite, a = 3.989 Å

Melting point			:	Does not melt congruently.

Density				:	7.015 g / cc

Thermal conductivity		:	0.17 w/m.k at 300k

Refractive index			: 	2.14

Sellenmeyer equation		:	(o2 -1 =3.591(2 / ((2 –(0.193) 2 )

(( in (m, from 0.4 – 1.06 (m )

Crystal growth method		:	Top seed flux growth

KaTaO3  Crystal Substrate Specs

Purity        			:	99.99%

Standard Sizes			:	10 mm x 10 mm x 0.5 mm

Common Orientation		:	(100) or (110),

Orientation tolerance		:	+ / - 0.5

Surface Finish			:	one or both faces epi-polished

Surface Roughness		:	<10 Å

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

KTaO3

Potassium Tantalate Single Crystals