LSAT (LaAlO3)0.3 (Sr2AlTaO6)0.7   is a newly developing crystal  with peroviskite structure and twin-free.  LSAT has excellent lattice match with high Tc superconductors and many oxide materials. LSAT has lower melting point and  can be grown by CZ technology at lower cost, therefore, it is expected to replace LaAlO3 and SrTiO3 as a common single crystal substrate for epitaxial oxide thin films for gain magnetic ferro-electronic and superconductive devices

|  | Typical Physical Properties |
| --- | --- |
| Chemical Formula | ( LaAlO3)0.3 (Sr2AlTaO6)0.7 or ( La0.18Sr0.82)(Al0.59Ta0.41)O3 |
| Crystal Structure | cubic: a = 3.868 Å |
| Growth Method | Czochralski |
| Density | 6.74 g/cm3 |
| Melt Point | 1840 oC |
| Thermal expansion | 10 (x10-6/ oC) |
| Dielectric Constant | ~ 22 |
| Color and Appearance | Colorless to light brown based on annealing condition No twin and domain visible |
| Standard Products |
| Epi -polished substrates <100>ori. ( 0.5o 1or 2 sides polished Ra < 8 Å | 2" dia x 0.5 mm 10 x 10 x 0.5mm Special size and orientation is available upon request 5 x 5 x 0.5 mm |

_____________________________________________________________________________________

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

LSAT crystal  Rocking curve

A New Twin-free Peroviskite Crystal

LSAT

( La0.18Sr0.82)(Al0.59Ta0.41)O3