# LaF3 Single Crystal

LaF3 is an excellent optical crystal applied as the lens, prism and window.  It has high transparency in the range of 0.2 ~ 10.5 micron wavelength.

|  | Typical Specifications |
| --- | --- |
| Crystal Structure | Trigonal: a= b= 7.190 Å, c=7.367 Å, (=(=90o, (=120o |
| Growth Method | Bridgman |
| Melting Point | 1493 oC |
| Crystal Purity | > 99.9% for undoped, Eu, Ca or Sr doping up to 5 mol% is available upon request |
| Crystal growth direction | < 0001 > |
| Density | 5.936 g/cm3 |
| Hardness | 4.5 (M) |
| Thermal expansion | 11.9 x10-6/ K // c 15.8 x10-6/ K // a |
| Thermal Conductivity | 5.1 W / m.k @ 300K |
| Optical Transmission range | Up to 10.5 micron wavelength (o : 1.63 (e: 1.597 |
| Standard LaF3 Crystal Boule and Substrates |
| Orientation | <0001> ( 0.5o |
| Polished surface | EPI polished on one side or two sides to Ra < 10 Å |
| Standard Boule | 10 ~ 50 mm diameter |
| Standard substrates | 10 mm dia. x0.5 mm 10 x 10 x 0.5 mm one side or two sides optically polished. |

### Special size and orientation are available upon request

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com