LiAlO2 is a potential substrate for III-V nitride thin films due to its excellent lattice mismatch to GaN ( <0.2% at  <100> ), chemical stability at high temperature and cost effective.  MTI can supply  LiAlO2 wafer up to 2” in diameter

|  | Typical Physical Properties |
| --- | --- |
| Crystal Structure | Tetragonal a=5.17 Å c=6.26 Å |
| Growth Method | CZ |
| Density | 2.2 g/cm3 |
| Melt Point | 1900 oC |
| Hardness | 7.5 (Mohs) |
| Color and Appearance | Transparent |
| As - grown boule <100> ori. | 2” in diameter. x 4” in length |
| Typical rocking curve | FWHM < 23” |

Special size and orientation are available upon request

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

LiAlO2 Crystal

A new crystal substrate for III-V Nitride films