LiGaO2 single crystal was grown in 1960's for laser application.  However,  it is found out that LiGaO2 is a potential substrate for III-V nitride thin films due to its excellent lattice mismatch to GaN ( <0.2% ), chemical stability at high temperature and cost effective.  MTI  has supplied high LiGaO2 crystal substrates for researchers since 1996, and has been improving crystal quality to meet blue LD application.

|  | Typical Physical Properties |
| --- | --- |
| Crystal Structure | Orthorhombic. a=5.4008 Å b=5.012 Å c= 6.379 Å |
| Growth Method | CZ |
| Density | 4.18 g/cm3 |
| Melt Point | 1600 oC |
| Color and Appearance | White to brown. No twins and inclusion |
| Standard Products |
| As - grown boule <100> ori. .± 0.5o | 30 mm dia. x 30- 50 mm length |
| As cut blank <001> ori. .± 0.5o | 20 x 20 x 0.7 mm thickness 10 x 10 x 0.7 mm thickness. |
| Epi -polished substrates <001 > ori. .± 0.5o 1 or 2 sides polished, Ra< 8 Å | 20 x 20 x 0.5mm 10 x 10 x 0.5 mm |

Special size and orientation are available upon request

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

LiGaO2 Crystal

A new crystal substrate for III-V Nitride films