MgO is an excellent  single crystal substrate for thin films of Ferro magnetic, Photo-electronic and  high Tc superconductor materials.  MTI uses a special arc melting method to grow high purity MgO crystal in sizes up to 2”x2”x 1” at lower cost, and employs CMP method to prepare high quality substrates with atomic level smoothness.

MTI also provides MgO substrate with as-cleaved surface. For some applications, as-cleaved MgO substrate gives better epitaxial thin film due to its more favorable surface conditions.

|  | Typical Properties |
| --- | --- |
| Crystal Structure | Cubic, a=4.216 ( |
| Growth Method | Special Arc Melting |
| Typical Purity: | >99.95% |
| Typical Impurity (ppm) | Ca ( 40, Al(15, Si(10, Fe(50, Cr ( 10, B(5, C ( 10 |
| Melting Point | 2852 oC |
| Crystal Purity | > 99.95% |
| Crystal cleavage plane | <100> |
| Density | 3.58 g/cm3 |
| Dielectric constant | 9.8 |
| Thermal expansion | 12.8 x10-6/ oC |
| Optical Transmission | > 90% @ 200 ~ 400 nm > 98 % 500 ~ 1000 nm |
| Crystal Prefection | No visible inclusions and micro cracking, X-Ray rocking curve available |
| Standard MgO Crystal Substrates Specification |
| Orientation | <100> ( 0.2o <110> and <111> ( 0.5o |
| Polished surface | EPI polished on one side or two sides to Ra < 10 Å |
| Standard Thickness | For ground blank: 1.0 mm ( 0.1mm Polished substrate: 0.5 mm ( 0.05mm As-cleaved substrates 0.8 mm( 0.2 mm |
| Standard Crystal Substrate | as-cut 2”x2”x 1.0 mm (2” x 1.0 mm 1”x1”x 0.8 mm (1” x 0.8 mm 10 x10x 0.7 mm | as polished 2”x2”x 0.5 mm (2” x 0.5 mm 1”x1”x 0.5 mm (1” x 0.5 mm 10 x10x0.5 mm | as-cleaved 10x10 x 0.8 mm 8 x 8 x 0.8 mm 5 x 5 x 0.8 mm |

### Special size and orientation are available upon request

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

0                 200              400              600               800             1000

# MTI MgO crystal optical transmission data

# X-Ray Rocking Curve of MgO Single Crystal

# Text boxes

MgO

Magnesium  Oxide Single Crystal

100

# Transmission %

90

80

Wave length  ( nm )