Nb doped SrTiO3 single crystal  has similar structure to pure SrTiO3, but become electric conductivity. Nb: SrTiO3 resistivity varies from 0.1 – 0.001 (-cm with Nb doping 0.01 ~ 0.001 wt %.  The conductive single crystal  substrates  provide an electrode for  certain thin film and device applications.  MTI supplies high quality and low cost Nb doped SrTiO3 substrate with the following specifications:

| Nb:SrTiO3 grade | A | B | C | D |
| --- | --- | --- | --- | --- |
| Nb Concentration ( wt %) | 1.0 | 0.7 | 0.4 | 0.10 |
| Resistivity ( ohm-cm) | 0.0035 | 0.0070 | 0.05 | 0.08 |
| Mobility ( cm2/Vs) | 9.0 | 8.5 | 8.5 | 6.5 |
| Standard Size and Orientation | 10x10x0.5mm, 5x5x0.5 mm |
| Surface finish | one or two sides epi polished, Ra < 8 Å |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

Nb:SrTiO3

## Niobium-Doped SrTiO3 Crystal