OTF-1200X3 Dual Zones Tube Furnace ( 2" )

with Split Cover up to 1200C

OTF-1200X3 is splitable three zones tube furnace, which can achieve faster heating up to 1200oC and create a different thermal gradient by adjust two zone temperature.  The furnace includes one 50 mm diameter fused quartz tube for immediate use.  Two precision temperature controllers are installed, which can provide 51-segments heating and cooling steps with +/- 1 oC accuracy with 15" length hot zone  Thermo-couple, Power cord and 2" quartz tube is included for immediate use.  Vacuum seal kit is available upon request.

Specifications:

| Power | KW | 5 KW |
| --- | --- | --- |
| Voltage | V | AC 220-240 Single Phase, 50/60 Hz |
| Max. Temperature | oC | 1200 |
| Continuous Temperature | oC | 1100 |
| Max. Heating Rate | oC /min | <= 20 |
| Suggested Normal Heating Rate | oC /min | 10 |
| Tube Size and Materials | mm | 2"Dia. x 40"L fused quartz tube included (50OD x 44ID x 1000L mm) |
| Heating Zone Length | mm | Three zones: each zone length 6" (152 mm) |
| Temperature Controllers |  | Three Digital Controller, and each has 51-segement programmable |
| Temperature Accuracy | oC | +/ - 1 |
| Heating Element |  | Fe-Cr-Al Alloy doped by Mo |
| Dimension | mm | 550 x 380 x 520 |
| Net Weight | Kg | about 50 |
| Warranty |  | One year limited (No warranty on quartz tubes and heating elements.) |
| Shipping package size after crating | inch | 45x45x35 |
| Shipping weight | lbs | 220 |

MTI Corporation

860 South 19th Street, Richmond, CA 94804, USA

Tel: 510-525-3070     Fax: 510525-4705      E-mail:  info@mtixtl.com       Website:  www.mtixtl.com