OTF-1200X  Quartz Tube Furnace Split Cover

3" dia. 1200oC with Stainless Steel Sealed flanges

OTF-1200X-3 is Tube furnace with Fe-Cr-Al alloy heating element and split cover, which can achieve faster heating and cooling rate.  The furnace is installed with 75 mm diameter quartz tube with a pair of smart stainless steel vacuum sealing flange, which allow to heat sample in vacuum or flowing gas.  Precision temperature controller can provide 51 segments heating and cooling steps with +/- 1 oC accuracy.

Specifications:

| Power | KW | 2.5 |
| --- | --- | --- |
| Voltage | V | AC 208-240 Single Phase, 50/60 Hz |
| Max. Temperature | oC | 1200 (<1 hour) |
| Continuous Temperature | oC | 1100 |
| Max. Heating Rate | oC /min | <= 20 |
| Suggested Heating Rate | oC /min | 10 |
| Tube Size and Materials | mm | OD: 76.2; ID: 71; Length: 1000, 3" Quartz tube ( included ) |
| Heating Zone length | mm | 440 ( single zone ) |
| Constant temperature zone | mm | 200 (+/-1oC) |
| Temperature controller |  | PID automatic control via current limiting phase angle fired the resistor with 51 steps programmable |
| Temperature Accuracy | oC | +/ - 1 |
| Vacuum Seal |  | two stainless steel flanges with vacuum gauge and valves |
| Vacuum Level ( by a mechanical pump ) | torr | 0.1 |
| Heating Element |  | Fe-Cr-Al Alloy doped by Mo |
| Dimension | mm | 550 x 380 x 520 |
| Net Weight | Kg | about 40 |
| Warranty |  | One year ( not including quartz tube) |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: 510-525-3070     Fax: 510525-4705      E-mail:  info@mtixtl.com       Website:  www.mtixtl.com