## Main Properties

Chemical Composition:						( PbMg 0.33 Nb 0.67)1-x: (PbTiO3)x

Structure:									R3m, Rhombohedral

Lattice:										a0 ~ 4.024Å

(pseudo-cubic, varies with composition )

Melting Point:									1280 oC

Density 										8.1	g/cm3

Piezoelectric Coefficient d33 						>2000 pC/N

Coupling Constant k33	(longitudinal mode)		>92%

kt	(thickness mode)			59-62%

k33’	(beam mode)				84-88%

Dielectric Constant	( (at 1kHz after poling)			4000 – 6000

Dielectric loss									tan( <0.9

Composition: 									near the morphotropic phase boundary.

Curie temperature:								135-150(C

Standard size									25× 25× 1mm3 plates along [001],

and other sizes are available on request.

Properties are somewhat dependant on the composition of  the solid solution so the choice of composition may require a compromise in desired properties.

______________________________________________________________

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

#### Lead Magnesium Niobate-Lead Titanate

PMNT SINGL CRYSTAL

A New Piezocrystal for Next-Generation Electromechanical Transducers