Lead tungstate ( PbWO4 ) is a new scintillating crystal discovered in 1990s. It is one of the most dense oxide crystal ( 8.3g/cm3), and is distinguished by its short radiation length ( 0.9 cm), small Moliere radius ( 2.19cm) and strong irradiation hardness. Its scintillation light output peaks between 450-550nm with a fast component decay time in the range from 2-20ns. After irradiation with g-ray, the degradation in the optical transmittance is not large up to 106 rad. PbWO4 is considered as a promising scintillation material for electromagnetic spectrometer in high energy, nuclear physics experiment as well as nuclear medicine.

## Main Properties

Crystal structure             			Tetragonal
Space group                   			I 41 /a
Lattice constant (Å )          			a = b = 5.416 ,	  c =  12.049 
Density  (g/cm3)                			8.28
Radiation length (cm)          			0.92
Molere radius (cm)            			2.19
Decay constant (ns)           			6/30
Peak emission (nm)             			440/530
Light output (%)               			0.5
Index of refraction           			2.16
Melting point (oC )            			1123
Hygroscopicity                			No
Cleavage                      				(101)

Crystal boule size					30 mm in diameter x 100 mm in length

______________________________________________________________

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

PbWO4

New scintillating crystal --  Lead Tungstate