Grade:  PG-SN

Method of Manufacturing: Hydrocarbon gas decomposition

Description: Pyrolytic Graphite (Substrate Nucleated) is a unique form of graphite manufactured by decomposition of a hydrocarbon gas at very high temperature in a vacuum furnace. The result is an ultra-pure product which is near theoretical density and extremely anisotropic. The material is grown onto a substrate giving it a layered composition. This also means it has different properties in different planes. In the C plane (across its layers) it has low thermal conductivity, acting as an insulator. In the A-B plane (with the layers) it has very high thermal conductivity, acting as a superb conductor. All values are taken at room temperature, unless noted otherwise.

| PROPERTY | US VALUE | METRIC VALUE |
| --- | --- | --- |
| Density | 0.079 | lb/in3 | 2.2 | g/cm3 |
| Flexural Strength – AB | 13000 | psi | 89.6 | mpa |
| Compressive Strength – AB | 15000 | psi | 103.4 | mpa |
| Compressive Strength – C | 25000 | psi | 172.4 | mpa |
| Shear Strength – AB | 1000 | psi | 6.9 | mpa |
| CTE – AB | 0.8 | in/in oFx10-6 | 0.5 | Microns/m oC |
| CTE – C | 11 | in/in oFx10-6 | 6.5 | Microns/m oC |
| Thermal Conductivity – AB | 232 | BTU/(h.ft2 oF/ft ) | 400 | W/(m2 . K/m) |
| Thermal Conductivity – C | 2 | BTU/(h.ft2 oF/ft ) | 3.5 | W/(m2 . K/m) |
| Resistivity (RT) – AB | 0.2 * 10-3 | ohm/inch | 0.5 * 10-3 | ohm/cm |
| Resistivity (1650C) – AB | 0.1 * 10-3 | ohm/inch | 0.3 * 10-3 | ohm/cm |
| Resistivity (RT) – C | 0.2 | ohm/inch | 0.5 | ohm/cm |
| Resistivity (1650C) – C | 0.1 | ohm/inch | 0.3 | ohm/cm |
| Oxidizing Atmosphere | 1200 | oF | 649 | oC |