SBN Single Crystal

Strontium-Barium Niobate (SrxBa(1-x)Nb2O6) SBN is an excellent optical and photorefractive material due to

its excellent photorefractive, electro-optic, nonlinear optic, and dielectric properties.  SBN crystal has a very

large electro-optic coefficient up to 1400 pm/V. and is potential crystal for new generation E-O devices

MTI provides SBN crystal up to 20x20x1.0 mm to support your research. Hope we can work together to

bring its cost down with increasing market demand

Typical Properties

| Chemical formula | (SrxBa(1-x)Nb2O6) 0.75>x>0.60 |
| --- | --- |
| Crystal structure | Tetragonal (4mm) a = 3.946 Å c = 12.46 Å |
| Melting point | 1500 oC |
| Density | 5.4 g/cm3 |
| Mohs hardness | 5.5 |
| Thermal conductivity | 0.006 W/cm*K |
| EO constants | (r33:460~1400pm/V) |
| High optical uniformity | (<1×10-4) |
| Dielectric constant | E11=450 E32=900 |
| Coercive field | (Ef:~0.25ｋV/mm |
| Curie Temperature | 70-80oC |
| Transmission range | 400 – 6000 nm |
| Absorption coefficient | 0.3cm-1 @ 0.44µm |
| Piezoelectric Coefficient | D33 = 130 m/V |
| Refractive index | no=2.312 ne=2.273 |

MTI Corporation

2700 Rydin Road, Unit D, Richmond,  CA 94804, USA

Tel: 510-525-3070     Fax: 510525-4705      E-mail:  info@mtixtl.com       Website:  www.mtixtl.com