SrLaAlO4 Single Crystal

SrLaAlO4 crystal  is a promising substrate material for high Tc superconductor film and other oxide films.

It has similar lattice constant to SrTiO3, but better quality and lower cost because of  CZ growth and lower

melting point)  MTI produces SrLaAlO4 crystal and substrate in house up to 35 mm

TECHNICAL DATA

| Crystal growth method | Czochralski |
| --- | --- |
| Crystallographic structure | Tetragonal Space group I4/mmm |
| Lattice constant | a = 0,3754 nm c = 1,2630 nm |
| Twinning structure | No |
| Colour | Colorless-Yellow |
| Density | 5,924 g/cm3 |
| Melting point | 1650°C |
| Hardness | at <001> : 3512 MPa at <100> : 6349 MPa |
| Thermal expansion coefficient | along a-axis : (7,55 ± 0,02) x 10-6 K-1 along c-axis : (1,71 ± 0,02) x 10-5 K-1 |
| Thermal conductivity | 8,82 W/mK@300 K 7,50 W/mK@450K |
| Dielectric constant | 17 |
| Dielectric loss tangent | 8 x 10-4 |
| Specific resistivity | 0,33 x 1015 Wm |
| Transmission range | 240 ÷ 6670 nm |
| Refraction index | 1,926 |
| Dispersion (nf-nc) | 0,002 |

Comparison of SrTiO3 - LaAlO3  - SrAlO4 Crystal

| Properties/Crystal | SrTiO3 | LaAlO3 | SrLaAlO4 |
| --- | --- | --- | --- |
| Structure | Cubic | Cubic at >435oC | Tetragonal |
| Lattice Constant | a=3.905 | a=3.821 A | a=b=3.756 A c= 12.630 |
| mismatch to YBCO a=3.9 | +0.12% | -2.0% | -3.7% |
| Dielectric Constant | ~300 | ~ 25 | ~ 17 |
| Grown Method | Vernuil | CZ | CZ |
| Melting point oC | 2100 | 2080 | 1650 |
| Density | 5.175 g/cm3 | 6.52 g/cm3 | 5.92 g / cc |
| Max. Crystal size | 30 mm dia. | 75 mm dia | 35 mm dia |
| Crystal quality | Wide rocking curve due to dislocation density | Visible twin due to phase transition around 400 oC | Narrow rocking curve, no twins, less defects |
| Crystal cost | Higher | Lower | Medium |

Typical Rocking Curves:  SrLaAlO4 vs SrTiO3

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

SrTiO3

Rocking Curve

FWHM:  1’30”

SrLaLO4

Rocking Curve

FWHM:  1’6”