STOICHIOMETRIC LITHIUM NIOBATE  ( SLN)

| Stoichiometric Lithium Niobate ( SLN) is grown by a patented technique with superior uniformity and composition. SLN features with high electro-optic and non-linear coefficients, It can be used in applications including E-O modulators, frequency doublers, Q-switches, waveguide substrates, etc… In recent years, periodically poled LN (PPLN) has opened the door to new and exciting applications such as all-solid-state laser source and RGB laser display. |  |
| --- | --- |

PROPERTIES  at 25 oC

| Chemical Formula | LiNbO3 |
| --- | --- |
| Composition | 49.8 mole%Li2O |
| Melting Point | 1160-1200°C incongruent melting |
| Crystal Structure | trigonal |
| Space Group | R3c |
| Point Group | 3m |
| Lattice Constant | a=5.14829 Å, c=13.8631 Å (hex) |
| Density | 4.612 g-cm-3 |
| Hardness | 5 moh |
| Thermal Expansion Coefficient | a=16.7x10-6, c=2.0 x 10-6 °C-1 |
| Curie Temperature | 1200 °C |
| Spontaneous Polarization | 0.71 Coul/m2 |
| Dielectric Constants | εs11=44, εs33=29, εT11=84, εT33=30 |
| Coercive field | <4.0 KV/mm |
| Bandgap | 3.9 eV |
| Transmission Range | 305 to 5500 nm |
| Refractive Index at 1064nm | no=2.2411, ne=2.1510 |
| NLO Coefficients at 1064nm | d31=-6.3, d33=-44 pm/V |
| Electro-optic Coefficients at 633nm (constant tension) | r13=10.4, r22=6.8, r33=38.3 pm/V |

Sellemier Equation (λ in μm)

Specifications of SLN Wafer

| Standard Orientation | Z-cut |
| --- | --- |
| Orientation Tolerance | ±0.5 ° or better |
| Typical Size, inch | 2” |
| Size Tolerances | ±0.5 mm for diameter, ±0.1 mm for thickness |
| Surface Quality | < 5A ( by AFM) |
| Single Domain and Polarity label | Available |

MTI Corporation

2700 D Rydin Road, Richmond, CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4705   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

SLN