# Automatic Section Saw (8") SYJ-200

# with complete accessories

SYJ-200 is a CE certified automatic diamond saw is designed for precision cutting all type of materials up to 3" diameter. The saw is equipped with 8" diameter diamond blade and touch-push panel to achieve automatic control. It is the perfect cutting tool for metallurgical, ceramic and materials research laboratories

SPECIFICATIONS

| Voltage and Power | 208V-240VAC, 600W 50/60Hz If you try to use at 110VAC, please order a 1000W transformer 110V-220V separately |
| --- | --- |
| Motor & Spindle | 1 HP high torque DC motor. 1" dia spindle and 2" flange to accept 6 - 8" dia diamond blade. Variable blade speed: 300-3500 RPM with screen touch control panel and digital display |
| Sample Stage & Controller | Quick clamp is included to make sample mount easy and fast. (click picture below-lefy) Automatic/manual control X and Y two axial motion via touch screen digitital panel ( click picture below right) Programmable Y and X axis advancement via LCD panel to achieve automatic cutting with 0.01 mm precision. X axis is for cutting feed which has Max. travel distance of 80 mm and adjustable speed from 1.0 mm/ minute to 20 mm/minutes. Max. cutting deepth ( or sample height ) 65mm Y axis is for controlling thickness of slices, which can be programmed up to 100 mm distance |
| Cutting Blade | Three 8" cutting blades are included and completed accessaories are included for immediate use ( see standard packing list ) One 8" diameter x 0.025" thickness x 1" arbor sintered diamond blade One 8" Dia x 0.04" t x1.26" arbor SiC Blade for cutting non-ferous metal one 8" Dia x 0.04" t x1.26" arbor Aluminum Blade for cutting ferous metal. |
| Water Cooling | Adjustable nozzles is installed for re-circulating coolant Protective splash cover with elec cooling duringtronic safety interlock installed Click the picture below to order an optional 6L coolant circulating tank which perfectly connects to SYJ-200. |
| Dimensions | 734mm x540mm x475mm |
| Shipping Weight | Shipping weight: 72 Kg |
| Warranty | Two Years Limited Warranty with life time support (not include the rusty part due to improper storage) |
| Certification | CE certified |
| Application Note | Must use anti-corrosion coolant during cutting to avoid rusting lead screw. Please never use water as coolant during cutting. You may select our LubeCool-150 lubricant as coolant, and order optional coolant circulation system at related product below, which will make the diamond blade cut more efficiently and prevent corrosion. Also, you can use W10-30 motor oil as coolant, which is available at any Auto store. Always clean machine, especially the lead screw by W40 lubricant after each use. Make sure the X,Y axes can move freely without blocking and rusting. |

MTI Corporation

860 South 19th Street, Richmond, CA 94804, USA

Tel: 510-525-3070     Fax: 510525-4705      E-mail:  info@mtixtl.com       Website:  www.mtixtl.com