Silicon Single Crystal Substrates

MTI supplies various Silicon single crystal substrates from 1" to 8" diameter.  The highest quality and lowest price are our commitments.  Please call toll free at 1-888-525-3070  for your every need on Si crystal wafers

Typical Properties

| Parameters / dopant | B doped | P doped | Undoped |
| --- | --- | --- | --- |
| Conductor Type | P | N | Instinct |
| Resistivity ( (.cm) | 10-3 ~ 40 | 10-3 ~ 40 | 102 ~ 104 |
| EPD (cm-2 ) | ( 100 | ( 100 | ( 100 |
| Vortex Defects | 0 | 0 | 0 |
| Oxygen Content ( /cm3 ) | ( 1 ~ 1.8 x1018 | ( 1 ~ 1.8 x1018 | ( 1 ~ 1.8 x1018 |
| Carbon Content ( /cm3 ) | ( 5x1016 | ( 5x1016 | ( 5x1016 |
| Boule Diameter | 1 ~ 8 ” | 1 ~ 8 ” | 1 ~ 8 ” |
| Standard Orientation | <100>, <111>, <110> | <100>, <111>, <110> | <100>, <111>, <110> |

Recommended Applications

| Wafer Resistivity ( (.cm) | < 0.05 | 1 ~ 5 | 6 ~ 12 | > 30 |
| --- | --- | --- | --- | --- |
| Application | epitaxial substrate | solar cell | IC, OE devices or sensors | special device or component |

MTI Corporation

2700 Rydin Road, Unit D, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4705   E-mail: info@mtixtl.com   Website: www.mtixtl.com