SiO2

Single Crystal Quartz Wafer

Single crystal quartz wafer is an excellent substrate for microwave filters for wireless communication industries.  MTI can provide high quality quartz wafers for both research and industries production at the lowest price.

|  | Typical Physical Properties |
| --- | --- |
| Purity Wt % | SAW grade: > 99.9 Optical grade: 99.99 |
| Crystal Structure | Hex. a= 4.914 ( c = 5.405 ( |
| Growth Method | Hydrothermal |
| Hardness | 7.0 Moh’s |
| Density | 2.684 g/cm3 |
| Melt Point | 1610 o C ( phase transition point: 573.1oC) |
| Specific heat | 0.18 cal/gm |
| Thermoelectric Constant | 1200 (V /o C @ 300 o C |
| Thermal conductivity | 0.0033 cal/cm/ o C |
| Thermal expansion (x10-6/ oC) | (11: 13.71 (33: 7.48 |
| Index of Refraction | 1.544 |
| Q value Acoustic velocity, SAW Frequency constant, BAW Piezoelectric coupling , | 1.8 x 106 min. 3160 ( m/sec ) 1661 ( kHz/mm ) K2 (%) BAW: 0.65 SAW: 0.14 |
| Inclusion | IEC Grade II |
| Standard Quartz Wafer Specifications |
| Orientation | Y, X or Z cut: Rotated to any value in the range 30o ~ 42.75o ( 5 min. Primary flat: orientation specified by customer ( 30 min Secondary Flat: orientation specified by customer. Seed: located in the center: width < 5mm, height > 66mm |
| Polished surface | EPI polished on one side or two sides to Ra < 10 Å Working Area: Wafer diameter minus 3 mm BOW: < 20 (m for 3” wafer and 30 (m for 4” wafer No chips out on working area. In the edge, chip width < 0.5 mm Pit and scratches: < 3 per wafer or < 20 per 100 wafers |
| Standard Thickness | 0.5 mm ( 0.05mm TTV < 5 (m |
| Standard Diameter | ( 2” (50.8mm ) ( 3” (76.2mm) ( 4”(100mm) (0.2 mm Primary Flat : 22 ( 1.5 mm (( 3” ) 32 ( 3.0 mm ( ( 4” ) Secondary Flat: 10 mm (1.5 mm |
| Production Capability | 20,000 wafer per month |

Special size and orientation are available upon request

________________________________________________________________________________

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com