SrTiO3 single crystal provides a good lattice match to most  materials with Perovskite structure.  It is an excellent substrate for epitaxial growth of HTS and many oxide thin films. SrTiO3 single crystal has also been used widely for special optical windows and as high quality sputtering target.

MTI has the full production line to manufacture first the high purity SrTiO3 powder, then the single crystal boules and finally the epi-polished substrates in many sizes. This allows us to provide SrTiO3 single crystal products with the highest quality and the lowest price to our customers the world over.

|  | Typical Physical Properties |
| --- | --- |
| Crystal Structure | Cubic, a=3.905 Å |
| Growth Method | Vernuil |
| Density | 5.175 g/cm3 |
| Melt Point | 2080 oC |
| Hardness | 6 ( Mohn) |
| Thermal expansion | 10.4 (x10-6/ oC) |
| Dielectric Constant | ~ 300 |
| Loss Tangent at 10 GHz | ~5x10-4 @ 300K , ~3 x10-4 @77K |
| Color and Appearance | Transparent (sometimes slightly brown based on annealing condition). No twins. |
| Chemical Stability | Insoluble in water |
| Standard Products |
| As - grown boule <100> | 30 mm dia. x 30- 50 mm length 22 mm dia. X 30 - 50 mm length |
| As cut blank <100> | 1" dia x 0.7 mm thickness 10 x 10 x 0.7 mm thickness. |
| Epi -polished substrates <100>, <110> or <111> ori. 1 or 2 sides polished, Ra< 7 Å | 1" dia x 0.5 mm 20 x20 x 0.5mm 10x10x0.5 mm |

# Text boxes

SrTiO3

Strontium Titanate Single Crystal

Vernuil growth

As grown STO

As annealed STO

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com