# RUTILE

Optical Grade TiO2 single crystal

Rutile ( TiO2) single crystal is one of the  most suitable materials for spectral prisms and polarizing devices such as optical isolators and beam displacers because it has a large birefringence with a high refractive index.   Compared to YVO4,  TiO2 crystal is more stable chemically and physically.   Our high quality rutile single crystal boule and polished components have been widely used for optical isolators and special prisms.

\

Transmittance Thickness        1mm				Refractive Index

|  | Typical Properties |
| --- | --- |
| Crystal Structure | Tetragonal a=4.5936 (, c= 2.9582 ( , |
| Growth Method | floating zone (FZ) |
| Melting Point | 1840 oC |
| Density | 4.26 g/cm3 |
| Hardness | Mohs 7 |
| Specific Heat capacity | 0.17 ( 25 oC) Cal. / (g. Deg) |
| Linear expansion Coefficient | a: 7.14x10-6 c: 9.19x10-6 |
| Refractive Index | n0 = 2.47 ne = 2.73 at ( = 1.3 (m |
| Transmittance | 0.5- 4.5 (m |
| Thermal optical Coefficient | d(/dT: a: -0.72 x10-6/K c: -0.42x10-6/K |
| Crystal boule dimension | ~25 mm dia x 35 mm length ( conical ) |
| Typical polished components | 2.6x2.6 x10 mm, 4x4x10 mm, 10x10x0.5 mm or any custom size Dimension: +/- 0.02 mm Roughness: < 5-10 Å |

The refractivity of RUTILE can be obtained from

the following equations ((, wavelength in ():

MTI Corporation

860South 19th Street,  Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4705   E-mail: info@mtixtl.com   Website: www.mtixtl.com