Ga Doped ZnO Single Crystal Substrate

Low conductivity ZnO single crystal substrates offer several advantages for both nitride and oxide based devices in base station wireless power amplifier applications. Low substrate defect density coupled with the isomorphic wurtzitic lattice with respect to GaN result in films that reward device manufacturers with better performance. The semi-insulating property of the substrate prevents parasitic currents in field effect transistors as well as permitting direct

Typical Properties

| Crystal Structure | Hexagonal: a= 3.252 å , c = 5.313 å |
| --- | --- |
| Growth Method | Melt |
| Hardness | 4 moh scale |
| Density | ~5.0 g/cm3 |
| Melt Point | 1975 oC |
| Band gap | 3.37 eV |
| Specific heat | 0.125 cal/gm |
| Conductivity | N type |
| Resistivity | 0.04 ohm-cm ± factor of 2 , N type |
| Carrier Concentration | 3.43 E+17cm3 |
| Thermal conductivity | 0.006 cal/cm/ oK |
| Thermal expansion | 2.90 x 10-6/oK |
| Dislocation Density | < 4 x 104 /cm2 |
| Availability of Standard Substrate |
| Orientation | <0001> |
| Polished surface | EPI polished on one side or two sides to Ra < 10 Å |
| Standard Size | 10x10 mm , 5 x 5 mm and Max. 1” diameter |
| Thickness | 0.35 mm, 0.5 mm and 1.0 mm |

MTI Corporation

2700 Rydin Road, Unit D, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4705   E-mail: info@mtixtl.com   Website: www.mtixtl.com