LiNbO3 Single Crystal

|  | Typical Properties |
| --- | --- |
| Crystal Structure | Hexagonal a=5.148 (, c= 13.863( |
| Growth Method | CZ |
| Melting Point | 1250 oC |
| Density | 4.64 g/cm3 |
| Curie Temperature | ~ 1160 oC |
| Hardness | 5 Mohs |
| Thermal expansion (x10-6/ oC) | (11: 15.4 (33: 7.5 |
| Index of Refraction | (o=2.286 (e=2.203 at 632.8 nm |
| Transmission wavelength | 0.4 ~ 2.90 ( |
| Nonlinear coefficient Electro-optical Coefficient | d33=34.45, d31=d15=5.95 d22=13.07 (pmV-1) (13=8.6, (22=3.4, ( 33=30.8, (51=28.0, ( 22=6.00 (pmV-1) |
| Transparency Range Transmissivity | 370 ~ 5000 nm > 68 % @ 632.8 nm |
| Sellmeier Equation ( ( in (m ) |
| (o2 (() = 4.9048 + 0.11768/((2 –0.04750) – 0.027169 ( (2 (e2 (() = 4.5820 + 0.099169/((2 –0.04443) – 0.021950 ( (2 |
| LiNbO3 Finished Components |
| Size | Any size below 4" diameter boule |
| Tolerance of size | Z-axis: ( 0.3 mm X-axis and Y-axis: ( 0.1 mm |
| Chamfer | Less than 0.5 mm at 45o ( 5o |
| Accuracy of orientation | Z-axis: < 5’ X-axis and Y-axis: < 10’ |
| Parallelism | < 10” |
| Finish | 10/5 scratch/dig |
| Flatness | (/8 at 632.8 nm |
| AR-coating | Reflectance < 0.2% @ 1064 nm |
| Wavefront distortion | < (/4 @ 633 nm |
| Extinction ratio | > 400:1 @ 633 nm, ( 6mm beam |

MTI Corporation

2700 D Rydin Road,  Richmond, CA 94804, USA

Tel: 510-525-3070  Fax: 510-525-4708   email: info@mtixtl.com    website:  www.mtixtl.com