LiTaO3 single crystal exhibits excellent electro-optical, piezoelectric and pyroelectric properties.  It has been used widely in pyrelectric device and color TV.  MTI specializes in optical grade LiTaO3 crystal featured with low impurity content, high performance and provides the most competitive price.

Typical Properties

Materials Purity:			> 99.995%

Crystal Structure:			Rhombohedral    space group 3M

Lattice Constant:			( Hex ) a = 5.154 (   c = 13.783 (

Melting Point:			1650 oC

Density:				7.45 g /cm3

Curie Point:			610 oC

Hardness:			5.5 - 6 Moh

Thermal Expansion:		( a= 1.61 x 10 -6 / k	 ( c= 4.1 x 10 -6 / k

Resistivity:			1015 (.m

Dielectric Constant:		(s11 / (0:  39 ~43		(s33 / (0:  42 ~43

(t11 / (0:  51 ~54		(t11 / (0:  43 ~46

Color:				colorless

Transmission Range                       0.4(5.0 (m

Refractive Index                              (o = 2.176  (e = 2.180 @ 633 nm

Standard Specifications of Crystal Boules and Wafers

| Item No | Products | Orientation | Standard Dimension |
| --- | --- | --- | --- |
| LTB | Crystal Boule | X ,Y or Z axis +/-1o | 2” dia x 50 mm L 3” dia x 50 mm L |
| LTW | EPI Polished wafer two sides polished Ra < 10 ( | X, Y, Z, or rotated Y cut with or without Flat | 10x10x0.5mm 2” dia x 0.5mm 3” dia x 0.5mm 3” dia x 1.0 mm |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

Optical Grade Lithium Tantalate

## LiTaO3 Single Crystal and Wafer

Optical Grade

We always keep standard wafer in stock for immediate delivery.  Special size and size of wafers are available upon request