# ND:YAG Crystal (Neodimium Doped Yttrium Aluminum Garnet)

Nd:YAG (Neodimium Doped Yttrium Aluminum Garnet) has been the most widely used laser crystal for solid-state crystal material.  Nd:YAG crystals are used in all types of solid-state lasers systems-frequency doubled continuous wave, high-energy Q-switched, and so forth. Compared with others laser crystals, its fluorescence lifetime is twice more than Nd:YVO4, and thermal conductivity is also better.

| Physical and Chemical Properties |
| --- |
| Chemical Formula | Nd:Y3A15O12 |
| Crystal Structure | Cubic Garnet |
| Lattice Constants | 12.01 |
| Concentration | ~ 1.2 x 1020 cm-3 |
| Melting Point | 1970 oC (2240K) |
| Density | 4.56 g/cm3 |
| Mohs Hardness | 8.5 |
| Refractive Index | 1.82 |
| Thermal Expansion Coefficient | 7.8 x 10-6 /K [111], 0 - 250 oC |
| Thermal Conductivity | 14 W/m /K @20 oC, 10.5 W /m /K @100 oC |
| Physical and Optical properties |
| Lasing Wavelength | 1064 nm |
| Stimulated Emission Cross Section | 2.8x10-19 cm-2 |
| Relaxation Time of Terminal Lasing Level | 30 ns |
| Radiative Lifetime | 550 ms |
| Spontaneous Fluorescence | 230 ms |
| Loss Coefficient | 0.003 cm-1 @ 1064 nm |
| Effective Emission Cross Section | 2.8 x 10-19 cm2 |
| Pump Wavelength | 807.5 nm |
| Absorption band at pump wavelength | 1 nm |
| Linewidth | 0.6 nm |
| Polarized Emission | Unpolarized |
| Thermal Birefringence | High |

MTI Corporation

860 South 19t hStreet, Richmond, CA 94804, USA

Tel: 510-525-3070  Fax: 510-525-4705 email: sales@mtixtl.com  Website:  www.mtixtl.com