Typical Properties

Chemical Formula:		(Zr,Y)O2 with  ZrO2 : Y2O3 = 92:8  ( 8 mol% Y2O3 stabilized )

Crystal Sructure:			Cubic, Face Centered, CaF2 type

Unit Cell	:			a = 5.125  Å

Density :				5.8 g  / cc

Purity:				99.99%

Melting Point:			2500 oC

Thermal Expansion Coeff	:	10.3 ppm / oC

Dielectric Constant:		27

Crystal  Growth Technique:	Flux Technique

Maximum crystal Size:		2" diameter

Standard substrate Sizes:	 	2" dia. x 0.5 mm thick, one side or two sides polished

1" dia. x 0.5 mm thick

10 mm x 10 mm x 0.5 mm

Standard Orientation:		(100),         (110) and (111) also possible

Orientation tolerance:		+ / - 0.5o

Surface Roughness:		<10 Å

MTI Corporation

860 South 19th Street, Richmond, CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4705   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

YSZ Single Crystals

Yttria stabilized Zirconia